J Wood Sci (2(K)5) 51:339-347 	© The Japan Wood Research] Socicly 2(K)5

DOI 10.1007/slOOS6-(X)4-066l-z

ORIGINAL ARTICLE

Anita Firmanti • Efendi Tri Bachtiar

Surjono Surjoknsumo • Kohei Komatsu • Shuichi Kawai

Mechanical stress grading of tropical timbers without regard to species

Received: March 12. 2(KM / Accepled: June 22. 2004

Abstract Some reports have shown that for single species the correlation between modulus of elasticity (MOE) and modulus of rupture (MOR) in bending is quite high. Tropical timbers consist of hundreds of species that are difficult to identify. This report deals with the mechanical stress grading of tropical timber regardless of species. Nine timber fepecies or groups of species with a total number of 1094 pieces measuring 60 x 120 x 3000mm, were tested in static betiding. The MOE was measured flat wise, while MOR was tested edge wise. Statistical analysis of linear regression with a dummy model and analysis of covariance were used to analyze the role of MOE and the effect of species on prediction of MOR. The analysis showed that using MOE as a single predictor caused under/overestimation for one or more species and/or ;groups of species. The accuracy of j prediction would be increased with species identification.' An allowable stress and reference resistance for species and/or groups of species were provided to compare with the prediction of strength through timber grading. The timber strength class for species and/or groups of species was also established to support the application of mechanical timber grading.

Key words Regardless of species • Mechanical stress grading • Tropical timbers • Allowable stress • Reference resistance

A. Firmanti

Research Institute For Human Settlements. Jl. Panvaungan-Cileunvi Wetan. Bandung 4000N. Indonesia

E.T. Bachtiar • S. Surjokusumo

Faculty of Forestry. Bogor Agriculture University. Kompleks IPB Darmaaa Bo«or 166X0. Indonesia

K. Komatsu • S. Kawai ( )

Research Institute Tor Sustainable Humanosphere. kvoto University. Uji 611-0011. Japan

Tel. +8I-774-3X-367J: Fax -SI-774-.nX-.167K e-mail: ska\vai(f'rish.kyoto-u.ac.jp