PENGGUNAAN TANIN KULIT

Acacia mangiwn Willd. PADA RESIN SISTEM

(Utiiization of Tannin from the Bark of Acacia trumgiwn Willd. In Resign System)

Lina Karlinasari, E. Roffael, Suminar S. Achmadi

ABSTRACT

The purpose of this study was to evaluate the character of tannin Acacia mangium barks and to compare dimensional stability and strength of MDF prepared using tannin from A. mangium in combination with commerciai UF, PF resin systems The bark was water extracted, in a water to bark ratio of 5:1 at temperature range of 60-70°C for 4 hour. Tannin-adhesive formulations prepared were: 1) UF-resin, 2) tannin extract + UF = 50% + 50%, 3) tannin extract + UF = 60% + 40%, 4) PF-resin, 5) tannin extract + PF = 50% + 50%, 6) tannin extract + PF = 60% + 40%. The extractive content of bark was 22.29%. The reactivity of extractives towards formaldehyde, as measured by Stiasny-method, was about 90.94%. The results indicted that the pH decreased with increasing of tannin concentration and the viscosity range of various formulation tannin-adhesives was between 2.5 to 30 poise. To a certain extent, the content of tannin in UF-resin systems has positive influences on thickness swelling, and modulus of rupture (MOR), white the internal bond seemed to decrease as a high amount of tamtin was used in UF-resin systems. Negative influence was observed in the thickness swelling and internal bond strength due to the use of tannin in PF-resin system. However, modutus of rupture (MOR) seemed to be positively affected Further works are needed for the improvement of tannin-UF and tannin-PF resin blends properties

Keywords: tannin, Acacia mangium Willd. UF and PF, resin system, MDF

# Footnotes

Sebagian dari paper ini disampaikan pada “The 4th International Wood Science Symposium” di Serpong, 2-5 September 2002

Staff Pengajar JTHH Fakultas Kehutanan IPB

Faculty of Forestry and Ecology, Goettingen University

Staff Pengajar Jurusan Kimia, FMIPA IPB