KOMB1NASI PERENDAMAN DALAM NATRIUM HIDROKSIDA DAN 
APLIKASI KITIN DEASETILASE TERHADAP KITIN KULIT UDANG 
UNTUK MENGHASILKAN KITOSAN DENGAN BERAT MOLEKUL
RENDAH
(Combination cf Soaking in Sodium Hydroxide and Chithin Deacetylase Apphcution on Shrimp Chit in in Producing Low Molecular Weight Chitosan
Aswita Emmawati1, Betty Sri Laksmi Jeni2, Yusro Nuri Fawzya3
I) Laboratorium Mikrobiologi Program Studi Teknologi Hasil Pertanian,
 Fakuilas Pertanian UniversitasMulawarman, JL Tanah Grogot Kampus Gunug Kelua Samarinda 75123. 2)
Fakultas Teknologi Pertanian Instuut Pertanian Bogor, 3) Pusat Riset Pengolahan Produk dan Sosiai Kkonomi Kelautann dan Perikanan Jakarta
Recieved 10 July 2007 accepted 27 July 2007

ABSTRACT
Thermostable chitin deacetylase produced by Bacillus K29-14 was used to produce chitosan from shrimp chitin. Chemical treatment before the enzyme application on chitin was conducted by soaking it in 60 % NaOH solution, which led chitin to swell and change the crystalline structure in order to allow the enzyme to penetrate and deacetylate it. The enzyme had performed high deacetylation degree (72-99 %) following soaking at 60-75 °C for 60-130 min. and then incubating with the enzyme at 55°C for 24 hours Deacetylation degree increased when soaking temperature in NaOH was increased or soaking time in NaOH was lenght, as well as by addition of enzyme. The chitosan had low molecular weight and viscosity, indicated that depolymerization was occured, so that resulted oligomer chitosan.
Keywords: chitin, chitosan, chitosan oligosaccharide, chitin deacetylase
PENDAHULUAN
Kitin merupakan polimer terbanyak kedua di alam, setelah selulosa. Secara luas, kitin terdapat sebagai komponen eksoskeleton Crustacea (seperti udang dan kepiring), Mo/lusca, serangga, arthropoda, cacing, dan dinding sel fungi. Kitin bersifat tidak ianit air dan hanya dapat lanit pada asam pekat, sehingga sulit diaplikasikan untuk berbagai keperluan praktis.
Deasetilasi kitin akan menghasilkan kitosan, yang dapat larut dalam asam encer, dan dalam bentuk oligomernya, dapat larut air. Pemanfaatan kitosan sangat luas, sebagai antibakteri, edible coating, film yang mudah terurai (biodegradable), untuk penyulingan air, penjemihan dan deasidifikasi sari buah, peng-emulsi, pengental,. penstabil, dan untuk enkap-sulasi. Kitosan juga dapat berfungsi sebagai serat makanan, menurunkan kadar kolestcrol dan absorpsi lipid scrta sebagai prebiotik (Shahidi et ah, 1999).
